## Slide 1: DEM simulation for suction filling
Kosei Yoshida1 Yuki Mori1
Kazuya Takabatake1 Mikio Sakai2*
1. Department of Nuclear Engineering and Management, School of Engineering, The University of Tokyo
2. Resilience Engineering Research Center, The University of Tokyo
[MS701C] 0161
Asian Pacific Congress on Computational Mechanics (APCOM)
Taipei International Convention Center, Taipei, Taiwan
20/12/2019
Notes: © Copyright PresentationGO.com – The free PowerPoint template library

## Slide 2: Backgrounds
The phenomenon that powder is drawn into the die region by the downwards motion of punch.
・Suction effect
[1] S. Jackson, I.C. Sinka, A.C.F. Cocks, 2006
・Powder compaction process
Powder compaction is widely used manufacturing process in above industries.
This process consists of 3 phases
・Previous Research
The effectiveness of suction effect has been examined mostly by the experiment.[1]
➀ Die filling
➁ Pressing
➂ Ejection
Important for productivity
Pharmaceutics
Metallurgy
Ceramics

## Slide 3: Objective
To reveal the mechanism of the suction effect in the die filling by employing numerical simulation.
Objective
Only by employing experiment, it’s difficult to obtain data inside of the die region.
Experiment
Numerical Simulation
Problem
1. Can’t pause powder flow
2. Difficult setting sensors
3. Difficult making certain experimental conditions
1. Can watch every moments
2. Can get many kinds of data
e.g.
・Pressure distribution
・Velocity distribution
3. Can make any conditions

## Slide 4: Numerical Methods
Advanced DEM–CFD Method[1]
Gas phase : Immersed Boundary Method[5]
Solid phase：Signed Distance Function[4]
DEM-CFD Method[2]
Boundary conditions
[1] H. Yao, et al., 2018
[2] Y. Tsuji et al., 1993
[5] Sun X., et al., 2017
Modeling of moving boundary with low calculation cost had been difficult.
Problem
Solid phase：Discrete Element Method[3]
Gas phase：Computational Fluid Dynamics
(Local volume averaged)
Drag force
[3] P. Cundall et al., 1979
[4] Y. Shigeto et al., 2013
Notes: Newton’s second law of motion.

## Slide 5: Conditions
Compare gravity filling with suction filling
Gas Phase | 
Viscosity | Pa・s
Density | 1 kg/m3
Solid Phase | 
Density | 1500 kg/m3
Spring Constant | 50 N/m
Coefficient of restitution | 0.9
Coefficient of friction | 0.3
Gas Phase | 
Viscosity | 
Density | 1 kg/m3
Solid Phase | 
Density | 1500 kg/m3
Spring Constant | 50 N/m
Coefficient of restitution | 0.9
Coefficient of friction | 0.3
Diameter | 250 μm
Number of particles | 500,000
System | Mono-dispersed
Grid size | 0.5 mm
Calculation time | 0.24 s
Time step | 2.0 × 10-6 s
Physical properties
Calculation conditions
Punch moves downwards
(500 mm/s)
Suction filling
Gravity filling
Unit : mm
Punch stays
at the bottom

## Slide 6: Results & Discussion
Gravity filling
Suction filling
0.020 s – much powder fed into the die region
0.060 s – powder concentrated along the center axis of die region and made much denser flow
In case suction filling,
0.180 s – completion of powder filling was earlier

## Slide 7: Results & Discussion
Drag
Pressure gradient
・Suction effect was produced by the pressure and drag force acted on powder
Influence of drag force is firstly found through this research.
Originality
Powder flux transition
Notes: I‘d like to emphasize

## Slide 8: Results & Discussion
Compare the 6 cases of the downward speed of punch. 200, 300, … , 700 mm/s . (6 cases)
Conditions
The natural phenomenon (the existence of the local minimum value) can’t be explained only by the influence of the pressure gradient and drag force.
Does the filling completion time becomes shorter as the punch velocity is higher ?
Powder flux transition
Natural phenomenon
: has local minimum value
Consider only the influence of pressure gradient and drag force
Powder filling time
Other factors which influence to the powder filling time exist.

## Slide 9: Results & Discussion
300 mm/s
500 mm/s
700 mm/s
0.040 s - much powder fed into the die region in the case of 500 & 700 mm/s
The existence of the local minimum value was observed in the simulation.
0.080 s - no clear difference of the powder filling rate among the 3 cases.

## Slide 10: Results & Discussion
As the punch speed was higher, the pressure gradient and drag force were stronger. And it created high flux in the initial stage.
① High flux in the initial stage
The times of flux increase end were different in each cases. The case 500 mm/s was the earliest.
② Flux increase at the final stage
①
②
The earliness of ➁ was correspond to the shortness of the filling completion time

## Slide 11: Results & Discussion
Bubbles prevented the powder flow into the die region
When punch speed is too high, bubble prevents the powder flux
After bubbles came out,
powder filled the die completely
② Flux increase at the final stage
Bubbles in the die
Originality

## Slide 12: Conclusions
In the moment of the punch start moving, both pressure gradient force and drag force act on powder. And they accelerates the powder.
1. Suction effect is produced
by drag force and pressure gradient
Punch movement suctions air into the die region, not only powder. It makes bubbles which prevent the powder feed into the die and delays the powder filling time.
2. When punch speed is too high,
bubble prevent the powder flux
Revealed the mechanism of suction effect in the die filling.
Drag
Pressure

## Slide 13: DEM simulation for suction filling
Kosei Yoshida1 Yuki Mori1
Kazuya Takabatake1 Mikio Sakai2*
1. Department of Nuclear Engineering and Management, School of Engineering, The University of Tokyo
2. Resilience Engineering Research Center, The University of Tokyo
[MS701C] 0161
Asian Pacific Congress on Computational Mechanics (APCOM)
Taipei International Convention Center, Taipei, Taiwan
20/12/2019
Notes: © Copyright PresentationGO.com – The free PowerPoint template library

## Slide 14: Validation of the method
Advanced DEM–CFD Method was validated in moving boundary system.[1]
[1] H. Yao, et al., 2018
Gas phase : Immersed Boundary Method[4]
Solid phase：Signed Distance Function[3]
Boundary conditions
Powder flow shape was correspond.
Final filled shape was also correspond.