## Slide 1
サクソン効果
ALLPPT.com _ Free PowerPoint Templates 、 Diagrams and Charts

## Slide 2
Parameters

## Slide 3: Physical properties
Gas phase | 
Viscosity | [Pa・s]
Density | 1 [kg/m3]
Solid phase | 
Hamaker constant | 0.0
Spring constant | 50 [N/m]
Coefficient of restitution | 0.9
Coefficient of friciton | 0.3
Gas phase | 
Viscosity | 
Density | 1 [kg/m3]
Solid phase | 
Hamaker constant | 0.0
Spring constant | 50 [N/m]
Coefficient of restitution | 0.9
Coefficient of friciton | 0.3

## Slide 4: Calculation conditions
Original particle size | 250 [μm]
Calculated particle size | 250 [μm]
Coarse grain ratio | 1
Number of particles | 500000
System | Mono-dispersed
Grid size | 0.5 [mm]
Calculation time | 0.2 [s]
Suction velocity | 300 [mm/s]
Courant Number | 0.2
Iteration limit | 1
Inverse of sound velocity | 0.1 [mm/s]

## Slide 5: Object size
20
40
40
20
10
50
10
[mm]

## Slide 6
Vacuum vs Air

## Slide 7: Vacuum vs Air
 | Case-Vacuum | Case-Vacuum
Analytic Model | DEM | DEM-CFD

## Slide 8: Vacuum vs Air
Case-Vacuum
Case-Air
Movie
-> Case-Vacuumの方が早く充填される。

## Slide 9: Vacuum vs Air
Case-Vacuum | Case-Air
sum | 146191 | 145008 | 
Number of partilces
in the die
層 | 5 |  | 31676 | 32622
 | 4 |  | 31197 | 32700
 | 3 |  | 31858 | 30383
 | 2 |  | 27387 | 25806
 | 1 |  | 24073 | 23497
-> Case-Vacuumの方が多くの粒子を充填できる。

## Slide 10: Vacuum vs Air
Layer
Chart: 層別粒子割合
| Vacuum | Air
1 | 24073 | 23497
2 | 27387 | 25806
3 | 31858 | 30383
4 | 31197 | 32700
5 | 31676 | 32622
-> Case-Vacuumの方がバランスが良く充填できる。

## Slide 11: Vacuum vs Air
結果・考察
・ Case-Vacuumの方が多くの粒子を充填できる
・ Case-Vacuumの方が早く充填される
-> ブロックが原因で流れ込みが進まないから
-> Case-AirではDie内に気泡がたまり、粒子の流入がブロックされる
・ Case-Vacuumの方がバランスよく充填できる
-> 下層粒子がブロックされることなく流れ込み続けるから

## Slide 12
Density Comparison

## Slide 13: Vacuum vs Air
 | Case-1 | Caes-2 | Case-3
Particle Density [kg/m3] | 1500 | 3000 | 4500

## Slide 14: Vacuum vs Air
Case-Vacuum
Case-Air
Movie
-> Case-Vacuumの方が早く充填される。

## Slide 15: Vacuum vs Air
Case-Vacuum
Case-Air
Movie-void fraction
-> Case-Vacuumの方が早く充填される。

## Slide 16
Case-Vacuum
Case-Air
Movie – void fraction

## Slide 17
Layer
Chart: 層別粒子数
| 100[mm/s] | 200[mm/s] | 300[mm/s]
1 | 20129 | 22542 | 23974
2 | 22576 | 25159 | 26392
3 | 28765 | 30313 | 30653
4 | 33207 | 33215 | 32134
5 | 37447 | 33510 | 31892

## Slide 18
Suction velocity [mm/s] |  | 
100 | 200 | 300
sum | 142124 | 144739 | 145045
Number of partilces
in the die
層 | 5 |  | 37447 | 33510 | 31892
 | 4 |  | 33207 | 33215 | 32134
 | 3 |  | 28765 | 30313 | 30653
 | 2 |  | 22576 | 25159 | 26392
 | 1 |  | 20129 | 22542 | 23974

## Slide 19
Velocity – Die内部の粒子数
Chart: Suction Velocity [mm/s]
| 100 | 200 | 300
Y の値 | 142124 | 144739 | 145045